## Slide 1: Robust d-wave superconductivity from the Su-Schrieffer-Heeger-Hubbard model: possible route to high-temperature superconductivity
arXiv: 2211.09143
Hao-Xin Wang
Group Meeting, Jan 14, 2023
Yi-Fan Jiang
Hong Yao
Acknowledgement:
H.-C. Jiang, S. Kiverlson, R.-Y. Sun, Y.-M. Wu, Z.-Z. Wu, X. Cai, Z.-X. Li

## Slide 2: Outline
Introduction

## Slide 3: The road to the microscopic mechanism for d-wave superconductivity
Cuprate phase diagram
[B. Keimer, et. al, Nature 2015]
Nearly forty years after the discovery of high- superconductivity, consensus about the theory has not been reached yet.
Recent numerical studies suggested that the simplest Hubbard model with strong Hubbard interactions in doping range relevant for hole-doped cuprates exhibits stripe order or phase separation but no d-wave superconductivity in the ground state.
[Mingpu Qin, el. al, PRX 2020]
[B.-X. Zheng, el. al, Science 2017]
Notes: It has been nearly forty years since the experimental discovery of high-temperature superconductivity. [J. G. Benordz and K. A. Muller, 1986]

## Slide 4: What more is needed beyond the Hubbard model?
SC with (electron doped)
S. Jiang, D. J. Scalapino, and S. R. White, PNAS 2021
D. N. Sheng, et. al PRL 2021
absent or weak SC (hole doped)
SC is also absent under hole doping even considering the third neighbor hopping . [S. Jiang, D. J. Scalapino, and S. R. White, PRB 2022]
D-wave states are discovered in doped J1-J2 spin liquid, and by imposing period-two stripe order. But these models are not realistic. [Hong-Chen Jiang and S. A. Kivelson PRL 2021; PNAS 2021]
The next nearest neighbor hopping
Notes: Relevent work for t2, Corboz iPEPS PRB 100, 195141

## Slide 5: Today’s key role: electron-phonon coupling
intertwined growth of the superconductivity and EPC
[Y. He, Z.-X. Shen et al.,Science (2018)]
Phase diagram of the Su-Schrieffer-Heeger model at half-filling
Xun Cai, Zi-Xiang Li, and HY PRL (2021)
Z. Han, S. A. Kivelson, and HY, PRL (2020).
Increasing experimental and theoretic researches indicate that EPC can be an essential ingredient in high-Tc superconductors, including cuprates and iron-based superconductors.
Notes: EPC drives the formation of Cooper pairs in conventional superconductivity.

## Slide 6: The Su-Schrieffer-Heeger-Hubbard model
The Hamiltonian of SSHH model:
electron site
phonon site
Xun Cai, Zi-Xiang Li, and HY, PRL (2021)
The model might be relevant to the physics of CuO2 plane considering B1g phonons.
Phonon frequency:
The dimensionless EPC constant:
with the bandwidth

## Slide 7: Limit analysis
At anti-adiabatic limit (, the effective electronic interaction mediated by phonons becomes instantaneous
J-term favors pairing on site or between nearest-neighbor sites.
We consider at finite 𝜆 under lightly doping
d-wave SC ?
BCS, s-wave SC

## Slide 8: Method: Density Matrix Renormalization group (DMRG)

## Slide 9
Phase Diagram
We employ a large-scale density-matrix renormalization group calculation for the SSHH model on four-leg ladders, and get the quantum phase diagram as a function of SSH electron-phonon coupling and Hubbard :
In the phase diagram, we fix the phonon frequency , and doping level concentration .
s-wave SC phase: dominant quasi-long-range on-site SC correlation and subdominant quasi-long-range charge density correlation;
stripe CDW phase: short-range SC correlation and long-range CDW ordering;
d-wave SC phase: dominant SC correlation with d-wave symmetry and subdominant charge-density correlation;

## Slide 10: s-wave state for finite and 𝑼=𝟎 (𝜆=0.3)
(b)
(c)
(d)
half-filled stripe state with wave length 4;
quasi-long range SC correlation with ;
Subleading quasi-long-ranged charge order
a spin gapped
Luther-Emery Liquid
Notes: Charge density profile on Lx = 48
superconductivity correlation
charge density correlation
spin correlation

## Slide 11
d-wave state for moderate EPC and 𝑼
Half-filled stripe state.
The amplitude of charge density wave (CDW), decay algebraically as system size increasing: a charge gapless state.
d-wave SC correlations decay in a polynomial form, with 1.
 pairing symmetry: plaqutte d-wave & ordinary d-wave
Spin gapped.
Notes: The wave length of charge density is , so-called half-filled stripe state.
The amplitude of charge density wave (CDW), decay algebraically as system size increasing, indicating a charge gapless state.
(d), (e), SC correlation on Lx=32 cylinder
The wave length of charge density is 4, so-called half-filled stripe state.
The amplitude of charge density wave (CDW), 𝐴_𝑐𝑑𝑤 decay algebraically as system size increasing, indicating a charge gapless state.
(d), (e), SC correlation on Lx=32 cylinder

## Slide 12: SC evolution from s-wave to d-wave
s-wave pairing
d-wave pairing
When fixing , i.e. = 0.3, and gradually increasing from zero, the onsite Hubbard repulsion naturally suppresses the onsite s-wave pairing tendency but leaves the bond d-wave pairing channel nearly unaffected.
Consequently, the system could be driven into a d-wave SC phase by sufficiently large, as shown in the last slides.

## Slide 13
stripe state
Renowned filled-stripe as in the Hubbard model
Short range SC correlation
The filled-stripe phase is stable against small

## Slide 14: Conclusions
From the state-of-the-art DMRG calculations, we have shown that the interplay between moderate SSH-type EPC and strong Hubbard 𝑈 on the square lattice can induce a d-wave SC state, which is a SC dominant Luther-Emery liquid state.
The d-wave SC states obtained for strong and moderate could have potential relevance for under- standing the d-wave SC in cuprates
Thank you for your attention!